MISSOURI DEPARTMENT TRANSPORTATION

CONSTRUCTION AND MATERIALS

Summary  for Preliminary Geotechnical Report* - - Form M-41

| Sheet | 3 | of | 3 |
| --- | --- | --- | --- |

| COUNTY: | Clark |  | ROUTE: | 61 |  | JOB NO.: | J3P0423 |
| --- | --- | --- | --- | --- | --- | --- | --- |

| HORIZON | SAMPLE DEPTH | CLASSIFICATION | DESCRIPTION | SHRINK FACTOR |
| --- | --- | --- | --- | --- |
|  |  | ASTM | AASHO |  |  |
| Composite | 0 – 4’ | CH | A-7-6-(19) | Brown fat clay, with some sand. | 1.13 |

| HORIZON | % PASSING | M.D., pcf | O.M % | PI | LL | STATION SAMPLED | LAB NO. ** |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | 3/4" | #40 | #200 |  |  |  |  |  |  |
| Composite | 100 | 99 | 95 | 97 | 21 | 36 | 53 | 655+00, 300’ RT. of C/L | 23DGL013 |

SOIL ASSOCIATIONS/SERIES Putnam silt loam Putnam-Mexico association

found from:

| Station: |  |  |  | Remarks: |
| --- | --- | --- | --- | --- |
| +605+40 | to | +616+00 |  | Shrinkage factors are estimated from average data, based upon typical properties of similar soils listed in the Geology and Soils Manual. This sample represents soil of glacial outwash, modified by weathering. These values are not intended for design purposes. |
| +647+50 | to | +656+50 |  |  |
| +712+00 | to | +739+70 |  |  |
|  | to |  |  |  |

*Description & soil properties are represented only as average or typical values.

**Test reports are on file with District Operations Engineer & District Geologist.