# Modified Bituminous Pavement Mixture (BP-2) NJSP-15-39A

***This JSP to be used when BP-2 is to be placed in 1-1/4 inch lift.***

**1.0 Description.** In addition to the requirements of Sec 401.3, the total aggregate prior to mixing with asphalt binder shall be in accordance with the following gradation requirements:

|  |  |
| --- | --- |
| **Sieve Size** | **Percent Passing by Weight** |
|  | **BP-2** |
| 1 inch | 100 |
| 3/4 inch | 100 |
| 1/2 inch | 99 - 100 |
| 3/8 inch | 90-100 |
| No. 4 | 60-90 |
| No. 8 | 40-70 |
| No. 16 | --- |
| No. 30 | 15-35 |
| No. 200 | 5-12 |

**2.0 Basis of Payment.** The accepted quantity Modified Bituminous Pavement Mixture (BP-2) shall be paid for at the contract unit price, as designated in the plans, for one of the following:

401-99.10, Misc. Modified Bituminous Pavement Mixture (BP-2) PG 64-22, per ton or

401-99.10, Misc. Modified Bituminous Pavement Mixture (BP-2) PG 70-22, per ton

**2.1 Price Adjustment for Fuel.** If the contractor accepts the option for fuel adjustment in the bid proposal, a fuel adjustment will be applied in accordance with Sec 109.14 for the type of pavement constructed.