# Macrotexture Surface for Ultrathin Bonded Asphalt Wearing Surface Requirement NJSP-17-04

**1.0 Description.** This work shall consist of producing a smooth and uniform milled surface in which an Ultrathin Bonded Asphalt Wearing Surface (UBAWS) will be placed.

**2.0 Construction Requirements.**

**2.1** After the existing pavement has been milled and other surface preparations as per Sec. 413.30.5.3 have been completed, the Contractor shall test the milled surface texture in accordance with ASTM E 965.

**2.2** The results of ASTM E 965 shall show a texture depth of any test area to have a maximum value of 3.0 mm.

**2.3**  The test areas shall consist of two tests, one in each traveled way lane, per mile or as directed by the engineer.

**2.4** All tests shall be observed by MoDOT personnel. The contractor shall provide all test result documentation to the engineer.

**3.0 Basis of Payment.** No additional payment will be made to the contractor as a result of this provision. Payment for compliance with this provision is considered included in the unit price of 622-10.01 Coldmilling Bituminous Pavement for Removal of Surfacing (3 Inches Thick or Less).