EPG GUIDANCE FOR SECTION 403

ASPHALTIC CONCRETE PAVEMENT with Balanced Mix Design and Performance Testing

This document was developed, and will be maintained, to clarify the intent of the specifications, reduce conflict in the QC/QA environment and improve uniformity of                contract administration across the state.

This is not a contract document and cannot be enforced as such. The Resident Engineer      always has the latitude to react in an appropriate way to job specific circumstances, but decisions should be consistent with the underlying intent of guiding specifications and policies.

For this discussion, QC refers to the contractor’s representative performing Quality Control testing. QA refers to MoDOT’s representative performing Quality Assurance testing.

Quality Control is a constant process that goes beyond taking samples required by random numbers.  Quality Control is the set of activities that control the quality of mix being produced and placed.  These activities include but are not limited to the required random number tests.  Quality Control also includes all informational tests on the materials and processes.

Informational Test refers to any testing performed by QC or QA that is not associated with a random number/sample location.  These tests are not to be used for PWL purposes.

QUESTIONS AND ANSWERS

- What sampling and testing procedures are required for the new BMD Specification?

- LOT Size – 6,000 Tons

- Maximum Sublot Size – 1,500 Tons

- (Each Lot requires at least 4 sublots)

| For Quality Control (QC) at one QC BMD Random Test |  |  |
| --- | --- | --- |
| TEST | FREQUENCY | MIN. NO OF SPECIMENS |
| QC - CTIndex | 1 Set per 3000 tons | 5 Compacted Specimens |
| QC - RTIndex | 1 Set per 3000 tons | 3 Compacted Specimens |
| QC – BMD Loose Mix Retained | 125 lbs per 3000 tons | Retained by Contractor |
| QA – BMD Loose Mix Retained | 125 lbs per 6000 tons | Retained by MoDOT |
| For Quality Control (QC) at one QC Volumetrics/AC Random Test |  |  |
| TEST | FREQUENCY | MIN. NO OF SPECIMENS |
| QC - % Asphalt Content | 1 Sample per Sublot | 1 Sample |
| QC - Gmm | 1 Sample per Sublot | 1 Sample |
| QC – % Air Voids | 1 Set per Sublot | 2 Compacted Specimens |
| QC – Volumetric/%AC Loose Mix Retained | 30 lbs per Sublot | Retained by Contractor |
| QA – Volumetric/%AC Loose Mix Retained | 30 lbs per 6000 Tons | Retained by MoDOT |
| For Quality Control (QC) at one TSR Random Test |  |  |
| TEST | FREQUENCY | MIN. NO OF SPECIMENS |
| QC – Tensile Str. Ratio (TSR) | 250 lbs loose mix per 12,000 tons | 8 Compacted Specimens |

| For Quality Assurance (QA) at one QA BMD Random Test |  |  |
| --- | --- | --- |
| TEST | FREQUENCY | MIN. NO OF SPECIMENS |
| QA - CTIndex | 1 Set per 12,000 tons | 5 Compacted Specimens |
| QA - RTIndex | 1 Set per 12,000 tons | 3 Compacted Specimens |
| For Quality Assurance (QA) at one QA Volumetrics/AC Random Test |  |  |
| TEST | FREQUENCY | MIN. NO OF SPECIMENS |
| QA - % Asphalt Content | 1 Sample per 6000 tons | 1 Sample |
| QA - Gmm | 1 Sample per 6000 tons | 1 Sample |
| QA – % Air Voids | 1 Set per 6000 tons | 2 Compacted Specimens |
| For Quality Assurance (QA) at one TSR Random Test |  |  |
| TEST | FREQUENCY | MIN. NO OF SPECIMENS |
| QA – Tensile Str. Ratio (TSR) | 250 lbs loose mix per project | 8 Compacted Specimens |

- 13x13x4.5-inch cardboard boxes are required for any QA retained loose mix and TSRs.  Boxes supplied by MoDOT since it is for QA testing.

- No container size requirement for QC retained samples.

- BMD Retained Samples

  - Contractors and MoDOT Districts retain BMD loose mix until passing QC and QA RT results are obtained at which time they can be disposed of.

      - BMD QA retained loose mix sent to MoDOT Central Lab for Hamburg testing if failing QC or QA RTIndex results.

      - BMD QC retained loose mix tested by Contractor for Hamburg testing if failing QC or QA RTIndex results.

- Volumetric/% AC Retained Samples

  - Contractors and MoDOT Districts retain Volumetric/% AC loose until comparable QC/QA results are obtained.

  - Retained material used for retest when QC/QA samples fail to compare.

- How are random numbers used with BMD sampling and testing? What goes with what?

  - 8 Different Random Numbers are generated based on tonnage.

| One Random Number Generated for Each of Below Tests |  |  |
| --- | --- | --- |
| Random Number | Test | Tonnage |
| 1 | QC - CT and RT Testing | 3,000 Tons |
| 2 | QC - Volumetrics and % AC | Sublot Size -Set by QC Plan |
| 3 | QC - TSR | 12,000 Tons |
| 4 | QC - Mat Density & Unconfined Longitudinal Joints | Sublot Size -Set by QC Plan |
| 5 | QA - CT and RT Testing | 12,000 Tons |
| 6 | QA - Volumetrics and % AC | 6,000 Tons |
| 7 | QA - TSR | Once per Project |
| 8 | QA - Mat Density & Unconfined Longitudinal Joint | 6,000 Tons |

- Can Mat Density and Unconfined Longitudinal Joints be Sampled at the Same Time?

- To limit work zone exposure, the same random number is used on Unconfined Longitudinal Joints as Mat Density as shown in Example 1 below.

Example 1 - If the random number longitudinal offset occurs within the limits of the unconfined joint, then an unconfined joint density core and a density core are taken at the same station.  1,500-ton sublot with a random number of 0.25.  1500 x 0.25 = 375 ton offset for both density and unconfined joint density core.

Unconfined Joint

375 Ton Offset

Confined Joint

- Example 2 shows how to handle unconfined joint density cores for a sublot when a portion of the sublot has a confined and unconfined joint.

Example 2 - When the random number station occurs at a station with a confined joint, the same random number is used to determine the location of unconfined joint.  1,500-ton sublot with a random number of 0.25.  1000 tons of sublot have a confined joint and 500 tons of sublot have an unconfined joint. For density core 0.25 x 1,500 = 375 tons offset.  For unconfined joint density core 0.25 x 500 = 125 ton offset.

Confined Joint						Unconfined Joint

125 Ton Offset

375 Ton Offset

Confined Joint

Note:  If only a small portion of the sublot contains an unconfined joint, it is at the discretion of the engineer to determine if an unconfined joint density core is required.  As a rule of thumb, if less than 200 tons has an unconfined joint, no core is required.

- Pay adjustments will only apply to the full width of the lane paved adjacent to an unconfined joint and not the entire sublot.

- What happens if random numbers fall at the same time?

  - Testing will be conducted in order received.  The contractor will be allowed to complete the first test, then immediately sample for the 2nd test.

  - The contractor can choose to hold on to loose mix sample for volumetric test until after the BMD testing is completed.

- If a random number falls at the end of the paving shift, can the sampling and fabrication of performance test specimens be moved up so that there is sufficient time for completing the sampling?

  - Yes.  Due to the amount of time and effort involved in BMD testing, the inspector needs to ensure there are at least 2 hours left in the shift at the point when BMD sample is taken so there’s enough time to fabricate the CT and RT test specimens.

  - Inspectors need to estimate a production rate for that day and estimate a 2-hour tonnage adjustment for the BMD testing.

- What BMD sampling methods are allowed?  Is sampling from multiple trucks allowed?

  - Follow AASHTO R 97 – Sampling Asphalt Mixtures

  - Beware of segregation when conducting sampling

  - Multiple truck sampling is not allowed.  It was determined that this was not needed.

- How much notice needs to be given for BMD testing at the plant?

  - MoDOT’s intent is to sample immediately when the tonnage is reached for the corresponding random number.  However, the following exception is permitted.

    - The contractor is in the middle of another test (informational or random).  The contractor is permitted to finish that test prior to starting this test.

- Can the contractor make plant adjustments after being given notification of a random number.

  - No plant adjustments shall be made after notification until the mixture is sampled that corresponds to the random number.  However, the following exception may be permitted.

    - If a random number falls at the very beginning of the day at plant start-up, the contractor should be allowed to make plant adjustments to improve quality and better represent the asphalt material of the entire sublot.  As a rule of thumb, MoDOT should allow 150 tons prior to issuing the random number at plant start-up.

- When is split sample testing utilized?

  - Split samples are used to ensure that the proper sampling, handling, and testing procedures are being followed by both QC and QA so that accurate results are obtained, and favorable comparisons are achieved.

  - In addition, if QA missed witnessing a QC sample; the QA may request to test the retained portion as a check since no inspection was done.

- How does MoDOT use informational test results taken outside of random numbers or general testing requirements outlined in the specification?

  - Used to test quality of isolated areas that QC/QA random tests do not capture.

  - Can be used to identify, quantify, and determine limits of any needed corrections.

  - Informational test has no impact on pay factors; except the total tonnage may be adjusted within the PWL calculations based upon any isolated areas identified. Informational test results shall not be used within the PWL calculations.

  - Due to the variability involved with plant start-up, MoDOT informational testing should be limited during the first 150 tons of the day.  More emphasis should be placed on getting adequate field density with minimized segregation rather than relying on volumetric testing results.

- Procedure for when QC and QA CTIndex results do not compare:

  - Favorable Comparison - QA and QC CTIndex results shall be within ± 30 points for SuperPave and +/- 60 points for SMA.

    - For the CTIndex test, if all QC and QA are greater than 80 for SuperPave mixes and greater than 190 for SMA mixes, then results are considered comparable regardless of difference.

    - QA RTIndex results shall be within ±15 percent of the QC testing that falls nearest.

  - Follow current procedures to check for sampling or testing errors by either party.

  - If no errors are determined, then QA result will be added to the QC results to include in the average.

  - CTIndex Reheated samples will not be used for dispute resolution due to the sensitivity of the test.

  - CTIndex test specimens older than 2 weeks will be considered invalid and shall not be used.

  - If RTIndex results do not compare, Hamburg testing shall be conducted on the QC/QA retained portion for comparison.

- Scenarios on how to pay for Section 403 mixes:

Assume Plan sheets show SuperPave on 4 ft inside shoulder and 2 ft of outside shoulder, with BP mix for remaining shoulder width.

SuperPave Inside Shoulder

SuperPave 2 ft of Shoulder

BP mix for Remaining Shoulder Width

SuperPave Limits

Ex. A - 18’ Pave Integrally

Example A – Where contractor paves wider with the Section 403 mix than is on the plans.

For example, paving 18 feet wide when the plans show the Section 403 mix is only 14 feet wide.  In this case the Section 403 mix extends four feet into what plans sheets show as shoulder mix.

    - Calculate quantity placed within the Section 403 limits and pay as Section 403 mix.

      - Density, % AC, VMA, % Av, TSR, and/or BMD incentive/disincentive pay would only apply to plan quantity placed within the Section 403 limits ~ 14 ft wide.

      - Section 401 specifications and pay factors apply to the remaining shoulder width area showing BP mixture.

    - Calculate quantity of Section 610 quantities on the 12-ft travel way for smoothness.

      - Smoothness incentive/disincentive would apply only to the 12-ft travel way.

  - What density testing applies within Example A?

    - The mat density within the travel way shall be in accordance with Sec 403.5.2 (92.5% -98.0% of Gmm).

    - Mat densities should always be taken within the travel way and not in the shoulder in accordance with Sec 403.5.2.2.

    - Otherwise, shoulder density shall be in accordance with Sec 403.15.3.

  - What density requirements apply to the shoulders?

    - The agency’s intent is to get the maximum amount of density on the shoulder as possible without damaging the underlying layers.  Specification says, “compacted to the specified density for the mixture”.

          - On new construction, shoulders should get the same compaction effort and rolling pattern as the travel way that meets the specified density (i.e., 92% of Gmm).

          - Often there is a need to relax density requirements on shoulders due to inadequate/unstable underlying layers.  Density requirements may be relaxed as approved by the engineer, and an acceptable rolling pattern established to achieve the optimum density for the shoulder.

          - Once rolling pattern is confirmed and the required or optimum shoulder density requirements are established, the density testing may be waived at the discretion of the engineer.

- Unconfined joint density core clarification:

  - An unconfined asphalt joint is a joint in an asphalt pavement that is not placed against a confining edge or structure.  The unconfined joint is created when an asphalt lift is being placed on an existing roadway without coldmillling the thickness of the asphalt lift.

SuperPave on 12-ft travel way and 2 ft of Shoulder

Ex. B – 1st Pass of Paving Operation at 14 ft wide.

Example B – Consider the 1st pass of asphalt lift being paved 14 ft wide that includes a 12 ft travel way and 2 ft of shoulder shown on the plans as SuperPave.  This creates two unconfined longitudinal joints, one near the centerline of the roadway and the other on the shoulder.

- Only the unconfined longitudinal joint near the centerline (because it is within the travel way) is held to the unconfined longitudinal joint density requirements within Section 403.23.4.1.

- There are no unconfined longitudinal joint requirements when located on the shoulders (outside the travel way).  These joints would get the same compactions effort as the shoulders, but not directly tested for density within 6 inches of the unconfined longitudinal edge.

- The plans show a ¾” coldmill with a 2” asphalt overlay.  Is the longitudinal joint considered confined or unconfined?

  - For any partial coldmilling (coldmilling depth less than asphalt lift being placed); the longitudinal joint is considered unconfined; and unconfined longitudinal joint cores would need to be cored and tested.

- If the contractor performs a corrective action on a longitudinal joint such as using a penetrating oil– are they eligible for full bonus?

  - As written, corrective action gives 100% pay.  Uncertain on the performance of RPE products in being as good or better than achieving full density.

  - If they mill and replace the sublot do, they get full bonus?

  - Yes, addressed in the specification.

- When new asphalt is required to be removed and replaced after paving operations have been completed, is new performance (CT, RT, & TSR) testing required for the replacement asphalt?

  - All removals and replacements over 6,000 tons need to be fully tested according to Section 403.

  - If new asphalt under 6,000 tons is removed and replaced for reasons other than failed performance testing, then additional performance testing is not required on that replacement mix. The replacement asphalt mix shall be accepted as small quantity.

  - If new asphalt under 6,000 tons is removed and replaced because of failed performance testing, then the replacement mix shall be performance tested again.

  - If the previous day/night’s production is required to be removed and replaced, then a new sublot shall be started with the replacement.

- Contractor equipment for CT index – hydraulic or screw driven?  Does the department have a preference?

  - No specification requirement,

  - Humbolt manufacturer customer service not good and test results were questionable.

- Binder source changes - 2 options:

  - Option 1 – If the virgin binder source changes but the virgin binder grade stays the same, the mix ID remains the same but an “A” gets added as is currently the protocol.

  - Option 2 – If the virgin binder grade changes or the mix is used for a different contract grade a new mix ID and JMF are required.

  - If the contractor wants to use a mix for two different contract binder grades, then a separate mix ID and balanced mix design test results are required for both contract binder grades.

- For example, a contractor wants to use a single mix design for both PG70-22 and PG76-22 then two mix design IDs will be issued.  Balanced mix design test results showing the mix meets both contract binder grades will need to be submitted as well. BMD testing results only, not entire volumetric analysis.

- Increasing the represented tonnage for BMD tests results at the end of a Project (CT, RT, & TSR):

  - The rule of thumb shall be that the last represented tonnage for BMD testing of a project can be increased by 1,500 tons the specified represented tonnage size.

    - Only the last CTindex, RTindex, & TSR represented tonnage of a project may be increased beyond specifications.

  - The last CT/RT represented tonnage of a project shall not exceed 4,500 tons.

  - The last TSR represented tonnage of a project shall not exceed 18,000 tons.

  - The last volumetric sublot of a project may be increased by 1,000 tons.

  - Staged construction (bridge ends, etc.) shall follow small quantities specification outlined in Section 403

- Small Quantity Clarification:

  - As defined in Section 403.20.1

  - When paving short sections of pavement (such as tie-ins) and the planned day’s paving production is less than 1,000 tons, the asphalt mixture may be accepted by small quantity methods.

  - If there is a small overrun of the planned small quantity amount that bumps the total quantities over 1,000 tons for the day, the exceeded tonnage may still be accepted by small quantities.

  - For quantities of 50 tons or less placed per day the asphalt mixture may be accepted by certification. No more than 250 tons of asphalt mixture may be accepted by certification per project.

- How to handle segregation identified by the PMTP:

  - The Veta file may be used as a tool by the RE/Inspector to locate areas of thermal segregation on the roadway. A visual verification of segregated areas on the roadway should be performed before any remedial actions are required. In general, if the segregation is not visible then remedial action is not warranted.

  - The nuclear density test method outlined in the specs should be a last result for the RE/Inspector but should be used if segregation is believed to be severe enough.

  - In an event of a dispute, segregated areas must be quantified by nuclear density method.

- PMTP Loss of Data due to equipment malfunction:

  - The contractor is required to make a reasonable effort to resolve the issue immediately. However, if the contractor is not able to resolve the issue immediately, they may continue paving without the possibility of receiving incentives for the PMTP data.

  - If the issue continues to last for multiple days, it is recommended that the RE talk to the manufacture to see how long a replacement can be provided to the contractor. If the contractor does not have a replacement PMTP by the date suggested by the manufacture, then the contractor shall not be allowed to continue paving until the PMTP is replaced.

- Nuclear density testing – clarification of how to implement TM-41 and when go to coring:

  - Contractor has the option to use nuclear density testing in lieu of coring for density bonus but QA would still require a core that the contractor would be required to cut.